# General

## SUMMARY

### Provide all labour, materials, and equipment for the installation of a decorative Microcement system, including surface preparation, primer, base coats, reinforcing fabric, finish coats, and topcoat as manufactured by Cementec and distributed by Durabond Products Limited.

## GENERAL REQUIREMENTS:

#### All conditions of the contract and Division 1, General Requirements apply to this section.

#### All work shall meet applicable codes and standards, the Occupational Health & Safety Act, manufacturer’s recommendations, and good building practice.

## Related sections and asubmittals

### Related Sections:

### Section 05 41 00 – Structural Metal Stud Framing

### Section 06 10 00 – Rough Carpentry

### Section 06 16 00 – Sheathing

### Section 07 62 00 – Sheet Metal Flashing and Trim

### Section 09 28 00 – Backing Board and Underlayment

### Submittals:

### Product Data

### Submit direct applied microcement system’s specifications and individual component data sheets to show compliance with design intent and installation instructions.

### Submit applicable approvals and/or evaluations for system/components.

### Shop Drawings

### Submit shop drawings per Division 1 requirements.

### Include dimensions, tolerances, details for terminations, drainage/venting, related/abutting components, and expansion/control joint locations.

### Samples

### Submit duplicate 300 mm x 300 mm (12” x 12”) representative colour samples for each finish prior to mock-up applications.

### Maintain approved sample on-site.

### Closeout Submittals

### Provide maintenance, repair, and cleaning procedures.

### Provide material and workmanship warranties per Section 1.10.

### Provide identification labels for colour batches, water-resistive barriers, base coats, finish coats, and reinforcing mesh.

## REFERENCES

### ASTM C109 – Compressive Strength

### ASTM D7234 – Pull-off Adhesion

### ASTM D2240 – Shore Hardnesss

### ASTM D4060 – Abrasion Resistance

### Manufacturer’s current technical literature and installation instructions

## QUALITY ASSURANCE

### Applicator must be certified by Durabond Products Ltd.

### Only approved personnel may install the Cementec Microcement System.

### Contractor shall be knowledgeable in proper installation and possess current Certificate of Installer. Work shall conform to good trade practices and manufacturer’s installation manual.

### Pre-installation meeting required with general contractor, design consultant, and applicator to confirm substrate, sequencing, and quality expectations.

### Provide minimum 1 m² mock-up for review and approval, showing colour, finish texture, and topcoat sheen.

## Delivery, storage, handling & protection

### Material must be supplied by the microcement system manufacturer in original unopened packaging with labels intact.

### Inspect materials upon delivery for damage; notify manufacturer in writing of unacceptable materials. Defective materials shall not be used.

### Store materials in dry, vented, weatherproof enclosure, off ground, out of direct sunlight, maintain ambient temperature between 5°C and 35°C.

### Protect freshly applied coatings from rain, weather, and damage until fully cured.

### Flashing and capping must be installed immediately or temporary protection provided; if not, notify Architect and General Contractor.

### Protect insulation boards from direct sunlight.

## project/site conditions

### Substrate must be approved by manufacturer, clean and free of contaminants (oil, dust, frost, efflorescence, etc.), and structurally sound.

### Substrate tolerance within 2 mm/m (0.25” per 10’).

### Report in writing all adverse conditions to consultant; correct before work begins.

### Apply only when ambient and substrate temps meet manufacturer specs; avoid wet, frozen, or frosted surfaces.

### Do no apply during or before inclement weather or if rain expected within 24 hours.

### Avoid direct sunlight and windy conditions during applications.

### Provide temporary enclosures and heat to maintain ambient temperature during and 24 hours.

### Do not apply finish coat where dust is generated.

### Protect from rapid evaporation in hot, dry weather. Consultant manufactuer for adverse conditions.

### All substrate cracks and joints must be secured and free from movement. Consult manufacturer for guidance on joint and crack treatment.

## design criteria

### Structural Design

### Design professional shall design the back-up wall in full compliance with the National Building Code (NBC) of Canada and/or applicable provincial or territorial building codes. Sufficient architectural plans and details shall demonstrate compliance.

### Supporting Substrate

### All substrates flat and plumb within 2mm/m (1/2” per 10’), per ASTM C 1397.

### Substrates free of surface contamination such as dirt, form release agents, efflorescence, oil, chalkiness.

### Substrates free of loose materials and cracks greater than 1mm (1/24”) in width.

# Products

## approved system

### Manufacturer: Cementec Microcement – Spain

### Distributor: Durabond Products Ltd. – www.durabond.com

## MATERIALS components

#### Primer:

#### Cementec Consolidator: For porous substrates.

#### Cementec Consolidator Forte: For non-porous substrates.

#### Base Coat:

#### Cementec BASE READY TO USE: Ready-mix decorative coating based on minerals and acrylic resins.

#### Reinforcing Fabric:

#### Fiberglass Mesh 2.6 oz/yd²: Alkaline-resistant fiberglass mesh suitable as minimum-grade reinforcement.

#### Finish Coats:

#### NOTE: Cementec Finish Coats can be applied in a variety of different methods to achieve various types of finish styles. Finish coat to be applied in manner approved by the architect/designer. Consult with Architect/Designer for finish. Finish to be approved by Architect/Designer.

#### Cementec Fino: Fine decorative finish for interior vertical/light-traffic areas.

#### Cementec Medio: Textured decorative finish for interior vertical/ and light-traffic areas.

#### Cementec High Traffic: For high traffic floors and high wear areas, abrasion resistant.

#### Primer for Sealer (Topcoat):

#### Cementec Techno Primer: Water-based impregnating product applied after finish coat and before topcoat.

#### Sealer – Topcoat:

#### Cementec Finish Forte: Two-component aliphatic polyurethane varnish available in matte, satin, or gloss finishes.

#### Cementec Finish Forte Plus: Moisture Curing aliphatic polyurethane varnish available in matte, satin, or gloss finishes.

##### External Fire Performance:  ASTM E648, Class I

##### Gloss Level: ASTM D-523, 10 (60 Degrees)

##### Coefficient of Friction: ANSI 326.3, 0.6

# Execution

## EXAMINATION

### Examine surfaces to receive the microcement system for defects that could affect execution and quality.

### Ensure substrate surfaces and applied base coats are dry, solid, and sound, free of ice, frost, oils, and other detrimental materials.

### Substrate tolerance within 2mm/m (0.25” per 10’).

### Verify flashing installed to divert water away from system.

### Report adverse conditions to consultant in writing.

### Do not start until satisfactory conditions are corrected.

### Commencement of work indicates acceptance of substrate conditions.

## PREPARATION

### Prepare substrates per manufacturer instructions.

### Thoroughly clean and wash surfaces, including base coats and existing coatings, removing all contaminants.

### Mask surrounding surfaces as necessary.

### Coordinate with other trades; ensure their components are in place prior to microcement application.

## APPLICATION

### General:

#### Use qualified, experienced installers.

#### Mix materials per manufacturer instructions.

#### Follow approved mock-up and shop drawings.

### Primer:

### Apply primer to all surfaces using a short hair microfiber roller and a brush (for corners and the most inaccessible places).

### First Base Coat and Reinforcing Mesh

### Apply first base coat on securely fastened trims and accessories.

### Install reinforcing mesh tight, straight, wrinkle-free.

### Apply base coat (~2mm) and immediately embed mesh fully, troweling from centre to edges.

### Final surface smooth and true within 3.2 mm/3m (1/8” per 10’).

### Sand dry surface with 100 grit paper to smooth out high spots and imperfections.

### Base coat shall be Cementec BASE READY TO USE in 1-2 coats.

### Base Coat:

### Ensure first base coat dry and clean.

### Lightly dampen in hot/dry weather if needed (do not saturate).

### Trowel-apply base coat (~2mm) over first base coat.

### Use wood/sponge float to remove high points after initial set.

### Final surface smooth and true within tolerance.

### Sand dry surface with 100 grit paper to smooth out high spots and imperfections.

### Finish Coat – 1st Coat:

### Apply within 3 days after primer.

### Match colour and texture to approved mock-up.

### Avoid surfaces to be caulked.

### Sand dry surface with 100 grit paper to smooth out high spots and imperfections.

### Finish Coat – 2nd Coat:

### Same as 1st coat instructions.

### Primer for Sealer (Topcoat):

### Apply Techno Primer (pre-sealer for topcoat) according to manufacturer’s instructions prior to topcoat application. Apply at 3 mils WFT.

### Sealer (Top Coat):

### For Low Traffic Areas apply finish FORTE aliphatic polyurethane varnish as topcoat, in strict accordance with manufacturer’s instructions. Apply at 3-5 mils WFT per coat. Apply 2nd coat within 24 hours of original application.

### For High Traffic Areas and Wet areas apply Finish FORTE PLUS aliphatic polyurethane varnish as topcoat, in strict accordance with manufacturer’s instructions. Apply at 3-5 mils WFT per coat. Apply 2nd coat within 24 hours of original application.

## [CLEANING

### Special Cleaning:

### Clean surfaces and work area of foreign materials caused by installation.

### Reinstate any soiled uncoated surfaces at installer’s expense.

## [PROTECTION

### Protect installed system from damage during construction.

### Protect materials from precipitation, freezing, heat, dust, and dirt during installation and curing.

### Protect adjacent materials from damage.

### Post warning signs during work and curing.

### Clean all surfaces after installation.

### Re-seal system every 3-5 years with a new sealer layer.

END OF SECTION